## Slide 1
Discrete Element Modelling and Micro-Computed Pore-Scale Hydrodynamic Behaviour of Open-Cell Foams
Research Group: Gas Turbine & Transmission
Research Division: Energy and Sustainability
1. Introduction
2. Research Approach
Figure 4: 2D horizontal slice after
processing in MatlabTM
Flow of fluids through open – cell metal foam is of great interest in many engineering application. These include sound absorption, car muffler design, aerospace, heat exchange equipment etc.
Pore – scale computational modelling is today the standard paradigm for availing ourselves the high fidelity porous materials models by linking its microstructural arrangement and macroscopic behaviour.
The non – destructive X – ray computerised micro – tomography (MCT) used at present provides an excellent two - dimensional high resolution images of the foam structure used for pore-scale computational modelling.
Total control of foam microstructural properties and reduced cost implication offer a high resolution two – dimensional slices obtained from discrete element simulation packing of spherical beads (DEM) a greater degree of choice in terms of replacing the MCT.
Figure 7 plots micro - CT computed, MTU (L-L) and DEM/CFD reduced pressure drop data against superficial velocity for varying degree of capillary radius (5.0 – 80um).
Within the range of pre-defined superficial velocity, The MTU (L-L) CFD computations agree reasonably well with DEM/CFD modelled data for a capillary radius of 20 – 30um with an approximate value of 7% (permeability) tolerance for a 1 bar infiltrated pressured foam (MTU) and DEM/DU2A (L-L) rc = 20um.
DEM data and X – ray micro – CT scanner have been used to provide a two – dimensional images of randomly-packed beds of monosized spherical beads and foam structures respectively for pore – scale laminar flow of fluid.
High-resolution MCT pore-scale computation provides a more literal description of the foam microstructural arrangement with a deviation of 2.3% (permeability) and 9.6% (Forchheimer coefficient) from reality whilst the easily and more flexible DEM structure yielded a deviation of 8.8 and 1.2% of both terms from reality.
www.nottingham.ac.uk
DEM was used to create randomly-packed beds of spheres (1.4 – 2.0mm and 2.0 – 2.5mm) using variable inter-particle friction to control the packing density, sizes and connectivity. Particle position and size data were then processed using MatlabTM to create 2D slices (as shown in Figures 3 and 4).
X-ray computerised micro – tomography scanner was used to provide a high resolution two – dimensional images of foam structures produced by infiltrating liquid aluminium (molten) into packed spherically shaped salt beads (NU spherical foam - G; 1.4 – 2.0mm) and pseudo-spherical hydro-soft packed salt (hydrosoft - foam - C; 2.0 – 2.5mm) beads at an infiltration pressure of ½ and 1 bar respectively.
SimplewareTM was used to import 2D slices and mesh the inter-particle spaces for simulation of the flow. The low velocity (Laminar flow) Navier-Stokes equation with velocity inlet, zero pressure outlet, symmetrical sides and internal wall boundary condition were solved in +FLOW module of SimplewareTM and COMSOL MultiphysicsTM.
A constant head permeameter was built to measure a discharge velocity (V) of water against a constant head (ΔH) for the laminar flow of fluid through the cross – section of a fitted foam matrix in a pipework as shown in Figure 5.
3. MCT and DEM comparison
5. Conclusions
Figure 9: Two – dimensional velocity profile plots of DEM and MCT computation.
Figure 7: Reduced pressure drop (106*Pa.s/m2)against superficial velocity (mm/s) for
DEM mono-sized (L-L) at rc = 5-80um
Figure 3: DEM simulation of the filling of a 35mm
diameter vessel with monosized beads
Figure 8 shows measured and CFD modelled pressure drop per unit length (Pa/m) against superficial velocity (mm/s) for the two foam structures.
The low inflow velocity of fluid against a fixated head loss recorded for NU spherical foam – G is an indication of low contacts (coordination number) between connecting pores compared to the hydro-soft foam – C.
Tolerable agreement between values obtained from the two pore-scale techniques and experimental data.
Otaru, A.J., Kennedy, A.R. & Morvan, H.P.
Department of Mechanical, Materials and Manufacturing Engineering, University of Nottingham, Nottingham,
NG7 2RD, United Kingdom.
Email:eaxao@nottingham.ac.uk
Figure 5: A constant head permeameter
Figure 2: Metal sponge (DEM)
Figure 1: Metal sponge (MCT)
DEM
Chart: Superficial velocity (mm/s)
| 0.1 | 0.2 | 0.3 | 0.42799999999999999 | 0.5 | 0.9 | 1.5 | 4.28 | 8 | 10 | 20 | 30 | 38.1
DU1 (L-L) - rc=5um | 0.9929 | 1.0119 | 1.0379 | 1.0779 | 1.1028 | 1.268 | 1.5666 | 3.0951 | 5.0919 | 6.1306 | 11.2177 | 15.669 | 19.2095
DU2* (L-L) rc=10um | 0.8985 | 0.91089 | 0.93003 | 0.96192 | 0.98279 | 1.1266 | 1.3953 | 2.8088 | 4.6853 | 5.6641 | 10.3155 | 14.7047 | 18.0816
DU2A (L-L) - rc=20um | 0.71653 | 0.7208 | 0.72736 | 0.73909 | 0.74722 | 0.80989 | 0.94242 | 1.7456 | 2.911 | 3.5405 | 6.6413 | 9.6241 | 11.9818
DU3 (L-L) - rc=45um | 0.27091 | 0.27168 | 0.27363 | 0.27757 | 0.28033 | 0.29998 | 0.33722 | 0.56341 | 0.91227 | 1.1071 | 2.1457 | 3.1577 | 3.9696
DU4 (L-L) - rc=80um | 0.1577 | 0.15797 | 0.15837 | 0.15906 | 0.15954 | 0.16323 | 0.17155 | 0.2585 | 0.36853 | 0.43083 | 0.75483 | 1.0884 | 1.3599
 | 0 | 5
DU2B (L-L) - rc=30um | 0.5007 | 0.50322 | 0.50709 | 0.51398 | 0.51878 | 0.55572 | 0.63477 | 1.1284 | 1.8684 | 2.2745 | 4.2449 | 6.2195 | 7.8189
MTU (L-L) | 0.85957 | 0.86336 | 0.86877 | 0.87807 | 0.88438 | 0.93165 | 1.0302 | 1.6301 | 2.511 | 2.9897 | 5.3329 | 7.5335 | 9.2222
4. Experimental validation
Figure 6: SEM images of the foams
Chart: Superficial velocity (mm/s)
MCT - G | 1
EXPT - C | 947.9762 | 2108.4298 | 3089.0947 | 5197.5245 | 12519.8232 | 17717.3477 | 22882.1833 | 31021.7028
DEM/CFD - C1 (1.0% shrink & rc = 10um) | 538.4632 | 1098.2388 | 2057.3804 | 6683.2881 | 16309.8864 | 22969.6234 | 30705.1529 | 37357.621
DEM/CFD - C2 (1.5% shrink & rc = 10um) | 345.1706 | 680.0012 | 1235.6505 | 3848.7278 | 9238.8159 | 12959.4236 | 17278.1261 | 20995.1164
DEM/CFD - C (1.0% shrink & rc = 12.5um) | 368.0945 | 759.8557 | 1478.0177 | 5424.5696 | 13713.5922 | 19298.6188 | 25529.2263 | 30996.647
EXPT - G | 0 | 947.9762 | 2108.4298 | 3089.0947 | 12519.8232 | 31021.7028
DEM/CFD - G (0% shrink & rc = 20um) | 0 | 657.0461 | 1421.6694 | 3506.8883 | 6463.2879 | 10338.6439 | 15146.425 | 20886.2464 | 27551.3738
MCT/CFD - C (Res=15um) | 494.2906 | 989.932 | 1675.9075 | 5118.3502 | 12209.4649 | 16967.974 | 22490.4582 | 27939.1207
MCT/CFD - C1 (Res=30um) | 547.7835 | 1107.1501 | 1852.6672 | 5887.6627 | 13818.9404 | 19386.7261 | 26174.0529 | 31744.6791
MCT/CFD - C2 (Res=60um) | 648.3958 | 1213.5516 | 2228.6017 | 7223.7985 | 17656.4394 | 24788.7934 | 32921.6206 | 39993.4364
Figure 8: Measured and CFD pressure drop per unit length
(Pa/m) against superficial velocity (mm/s).
MCT
k0, NU spherical =1.390*10-09m2
k0, Hydrosoft =4.87*10-09m2
AO would like to acknowledge the University of Nottingham for its 2014 Dean of Engineering Scholarship for International Excellence.